CHARACTERIZATION OF THE EXTRACTED MACROMOLECULES FROM AQUACULTURE PROCESSING WASTE

### Grammatical should be in lower case like these -

Characterization of The Extracted Macromolecules from Aquaculture Processing Waste

### Abstract

Aquaculture, the cultivation of aquatic organisms such as fish, crustaceans, mollusks, and aquatic plants, has rapidly become a corner stone of global food production (Little et al., 2016). The rise of aquaculture responds directly to the increasing global demand for seafood alongside the ongoing depletion of wild fish stocks, necessitating more sustainable methods to meet the nutritional requirements of a growing population. However, such rapid expansion concurrently presents a range of environmental and economic challenges, notably in the management and disposal of aquaculture processing waste. The processing of aquatic organisms results in significant waste generation including fish skin, viscera, scales, and exoskeletons.The traditional handling of aquaculture processing wastes, such as fish skin, viscera, and exoskeletons, often involves their disposal or use in low-value applications, contributing to environmental pollution and resource wastage. By focusing on the extraction and characterization of bioactive macromolecules from these wastes, this study not only provides a solution to waste management challenges but also opens up new avenues for the creation of high-value products. The valorization of aquaculture processing waste into valuable resources aligns with global sustainability goals, offering an environmentally friendly alternative to conventional waste disposal methods. The bioactive compounds derived from this research; including gelatin, proteolytic enzymes, and chitosan, have a wide range of applications in biomedicine and biotechnology. Their extraction and subsequent utilization could lead to the development of innovative products that enhance human health, improve industrial processes, and contribute to environmental sustainability.

### Keywords: Aquaculture, Fish Skin, Viscera, Exoskeletons

### Write more keywords in a to z order.

### Introduction:

Aquaculture, the cultivation of aquatic organisms such as fish, crustaceans, mollusks, and aquatic plants, has rapidly become a corner stone of global food production (Little et al., 2016). The rise of aquaculture responds directly to the increasing global demand for seafood alongside the ongoing depletion of wild fish stocks, necessitating more sustainable methods to meet the nutritional requirements of a growing population (Anderson et al., 2017). This burgeoning industry has substantially contributed to economic growth, showcasing substantial gains over recent decades. However, such rapid expansion concurrently presents a range of environmental and economic challenges, notably in the management and disposal of aquaculture processing waste. The processing of aquatic organisms results in significant waste generation, including fish skin, viscera, scales, and exoskeletons (Coppola et al., 2021). Unfortunately, these by-products are often viewed as low-value resources, leading to their common disposal or relegation to secondary applications such as animal feed, fertilizers, or landfills. This mismanagement exacerbates issues of environmental pollution and resource inefficiency (Fraga-Corral et al., 2022;  Rebouças et al., 2023).

### The underutilization of aquaculture by-products represents not only a significant environmental challenge but also a noteworthy economic opportunity. This duality has spurred increased interest in discovering sustainable and economically viable methods to convert waste materials into high-value products (Choudhury et al., 2022). Recent advancements in biotechnology have illuminated the considerable untapped potential of these by-products, revealing that aquaculture processing waste is rich in bioactive macromolecules including proteins, enzymes, and polysaccharides, each possessing a diverse array of functional and industrial applications (Al Khawli et al., 2020).

This is highly significant as it addresses the urgent need for sustainable practices within the rapidly expanding aquaculture industry. The traditional handling of aquaculture processing wastes, such as fish skin, viscera, and exoskeletons, often involves their disposal or use in low-value applications, contributing to environmental pollution and resource wastage (Guru, G. S., Pandey, C., Ali, M., & Thiske, S., 2024). By focusing on the extraction and characterization of bioactive macromolecules from these wastes, this study not only provides a solution to waste management challenges but also opens up new avenues for the creation of high-value products. The valorization of aquaculture processing waste into valuable resources aligns with global sustainability goals, offering an environmentally friendly alternative to conventional waste disposal methods. The bioactive compounds derived from this research; including gelatin, proteolytic enzymes, and chitosan, have a wide range of applications in biomedicine and biotechnology. Their extraction and subsequent utilization could lead to the development of innovative products that enhance human health, improve industrial processes, and contribute to environmental sustainability.

Highlighted are not cited.

The characterization of bioactive macromolecules derived from aquaculture processing waste is a critical step in understanding their structural, physicochemical, and functionalproperties (Reddy et.al.,2012; Maschmeyer et.al.,2020). As global aquaculture production continues to expand, the efficient utilization of its by-products has gained considerable attention for both economic and environmental sustainability (Stevenset.al. 2018). Aquaculture processing waste, which primarily consists of fish skin, viscera, and crustacean exoskeleton, represents a rich source of valuable biomaterials such as gelatin, proteolytic enzymes, and chitosan (Maschmeyer et al., 2022). These bioactive macromolecules exhibit unique biochemical and structural attributes that make them suitable for applications infood, pharmaceutical, biomedical, and environmental industries (Udayakumar et al., 2021). However, their industrial feasibility and functional efficacy largely depend on precise characterization, which ensures their stability, quality, and performance in targeted applications (Reddy et al., 2012).

This chapter presents a systematic investigation into the physicochemical, biochemical, and structural properties of macromolecules extracted from aquaculture processing waste. The primary focus is on gelatin extracted from fish skin, proteolytic enzymes (trypsin and chymotrypsin) isolated from fish viscera, and chitosan obtained from crustacean exoskeletons. Each of these biomolecules possesses distinct functional characteristics that make them highly valuable in various domains. Gelatin, for instance, is widely used as a gelling and stabilizing agent in food and pharmaceuticals, whereas proteolytic enzymes play a crucial role in biocatalysis, protein hydrolysis, andtherapeuticapplications. Chitosan, adeacetylated form ofchitin, has garnered significant interest due to its biocompatibility, antimicrobial properties, and adsorption efficiency, making it a promising candidate for biomedical, pharmaceutical, and environmentalapplications.

Highlighted are not cited.

To establish a comprehensive understanding of these macromolecules, advanced analytical techniques are employed for their characterization. Fourier-transform infrared spectroscopy (FTIR) is utilized to elucidate the functional groups and confirm the molecular structures of the extracted compounds. Scanning electron microscopy (SEM) provides detailed insights into their microstructural morphology, which is crucial for applications in biomaterials, drug delivery, and tissue engineering (Shah et al., 2018).

Green highlighted not relevant to you’re cited line.

In addition, biochemical assessments, including protein content analysis, enzymatic activity determination, and degree of deacetylation measurement, contributesto understanding their efficacy and stability under various conditions. Beyond structural characterization, this chapter also explores the functional properties of these bioactive macromolecules, which play a pivotal role in their industrial applications. The gelling, emulsifying, and stabilizing capacities of gelatin are analyzed, while the catalytic efficiency of trypsin and chymotrypsin under different environmental conditions is evaluated to determine their optimal activity range. Furthermore, the water absorption capacity, adsorption efficiency, and antimicrobial potential of chitosan are examined, emphasizing its versatility in biomedical and environmental remediation applications (Rawte, K., et. al., 2024). These assessments collectively provide a scientific foundation for optimizing the utilization of these biomolecules in diverse sectors (Stevens et al., 2018).

Highlighted are not cited.

Materials and Methods:

### CharacterizationofExtractedCompounds:

The extracted bioactive macromolecules (gelatin, chitosan, and proteolytic enzymes) were characterized to determine their physicochemical, biochemical, and structural properties. These analyses ensured the quality, functionality, and potential applications of the compounds.

Highlighted are not cited.

### PhysicochemicalProperties:

pH Measurement:

The pH measurement of gelatin and chitosan solutions was conducted to ensure their suitability for further experiments. A 1% (w/v) solution of each material was prepared by dissolving the required amounts of gelatin and chitosan in distilled water under continuous stirring until completely dissolved. The pH of the resulting solutions was measured using a calibrated digital pH meter. Before performing the measurements, the pH meter was calibrated with standard buffer solutions of pH 4.0 and 7.0 to ensure accurate and reliable readings.

Highlighted are not cited.

The calibrated meterwas then carefullyused to recordthe pH values of the prepared solutions (Goudie et al., 2023).

### MoistureContent:

Themoisturecontentofthesamplewasdeterminedtoevaluateitswaterretention properties. A known weight of the sample was accurately measured and placed in a hot air oven set to 105°C. The sample was dried at this temperature until a constant weight was achieved, indicating the removal of all moisture. After drying, the sample was weighed again to record its final dry weight (O’Kelly, 2004). The moisture content was then calculated using the following formula

This calculation provided the percentage of moisture present in the sample based on the difference between its initial and final weights.

### Ash Content:

Theash content ofthesamplewasdeterminedtoanalyzeitsinorganicresidueafter complete combustion. A pre-weighed amount of the sample was placed in a clean, dry crucible and incinerated in a muffle furnace at 600°C for 4–6 hours, ensuring complete combustion of the organic components. After incineration, the crucible containing the residue was cooled to room temperature in a desiccator to prevent moisture absorption and then weighed (Bjurström et al., 2014). The ash content was calculated using the following formula:

This calculation provided the percentage of inorganic material present in the sample based on the residue remaining after incineration.

### ResultsandDiscussion:

The comprehensive characterization of bioactive macromolecules extracted from aquaculture processing waste provides significant insights into their physicochemical, biochemical, structural, and thermal properties. These findings reinforce their potential applications across various industries, including pharmaceuticals, biomedical engineering, and food technology.The following sections present an in-depth analysis of these macromolecules based on the data obtained from experimental characterization techniques.

### Characterization of Extracted Macromolecules from Aquaculture Processing Waste:

The extracted macromolecules, including chitin, chitosan, gelatin, trypsin, and chymotrypsin, underwent systematic characterization to assess their fundamental properties.The diverse physicochemical, biochemical, and structural attributes identified in this study highlight their prospective industrial applications (Tables 1–.5).

Mention table no. 05

### PhysicochemicalPropertiesofBioactiveMacromolecules:

The physicochemical analysis revealed substantial variations among the macromolecules, influencing their functional applications (Table 1). Chitin exhibited a near-neutral pH (7.3 ± 0.3), while its derivative, chitosan, displayed a slightly acidic pH (6.1 ± 0.4). Gelatin was more acidic (5.3 ± 0.2), which aligns with its wide applicability infoodandpharmaceutical formulations. In contrast,trypsinandchymotrypsinexhibited alkaline pH optima (7.5–8.5 and 7.8–8.2, respectively), reinforcing their effectiveness in protein hydrolysis applications.

Chitinwasinsolubleinwater,whereaschitosandemonstratedasolubilityof83.45 ± 6.41%, highlighting its suitability for biomedical applications. Gelatin, trypsin, and chymotrypsin exhibited full solubility (94.2–100%), thereby enhancing their enzymatic efficiency. The thermal degradation analysis revealed high stability for chitin (311.23 ± 23.54°C) and chitosan (246.45 ± 30.54°C), signifying their durability in material applications. Conversely, gelatin degraded at a lower temperature (126.62 ± 18.42°C), making it an ideal candidate for temperature-sensitive applications. The molecular weights of chitin (743 ± 21.3 kDa) and chitosan (634.47 ± 23.66 kDa) impacted their viscosity and bioactivity, influencing their industrial relevance.

### BiochemicalPropertiesofExtractedMacromolecules:

Biochemical characterization (Table 2) indicated high protein content in gelatin (85–95%), trypsin (85–90%), and chymotrypsin (88–93%), affirming their suitabilityforpharmaceuticalandnutritionalapplications.Incontrast,chitinandchitosan contained minimal protein (<1%), highlighting their purity and potential for biomaterial applications. Gelatin exhibited a slightly higher lipid content (0.1–1.0%), whereas other macromolecules had negligible lipid levels.Enzymatic activity analysis demonstrated high catalytic efficiencies for trypsin (8,000–12,000 U/mg) and chymotrypsin (8,500–11,500 U/mg), establishing theirefficacy as biocatalysts in protein hydrolysis. Chitosan exhibited significantantimicrobial activity, with a Minimum Inhibitory Concentration (MIC) of 50–200 μg/mL, reinforcing its potential role in food preservation and biomedical applications. Gelatin's gel strength (200–300 Bloom g) was notably high, making it a valuable component in pharmaceutical and food formulations. The isoelectric points (pI) varied, with chitosan (6.2–7.0) being near neutral, while trypsin (10.5–11.0) and chymotrypsin (8.5–9.0) had alkaline pI values, enhancing their enzymatic performance.

### StructuralCharacterizationUsingFTIRAnalysis:

Fourier Transform Infrared (FTIR) spectroscopy confirmed the presence of key functional groups (Table 3, Fig..1). Broad O-H and N-H stretching peaks (3400– 3450 cm⁻ ¹) were detected across all biomolecules, indicating strong hydrogen bonding andproteininteractions.TheamideI(1650–1660cm⁻¹)andamideII(1550–1580 cm⁻ ¹) bands confirmed protein presence in gelatin, trypsin, and chymotrypsin. C-H stretching (2900–2960 cm⁻ ¹) signified protein-lipid interactions, particularly relevantfor proteolytic enzymes. The C-O-C stretching (1050–1080 cm⁻ ¹) identified in chitinand chitosan verified their polysaccharide backbone.

### MorphologicalAnalysisUsingScanningElectronMicroscopy(SEM):

### Scanning Electron Microscopy (SEM) revealed distinct microstructural characteristics(Table.5, Fig..2).

Mention table no. 05

### Chitinexhibitedacompact,fibrousmorphologywith rough surfaces, indicative of its rigidityand biodegradability. Chitosan showed a porous, flakystructure,enhancingitsbioactivityandadsorptionefficiency.Gelatindisplayedasmooth, film-like appearance, supporting its applications in biomedicine. Trypsin and chymotrypsin presented globular structures, essential for their enzymatic functionality.

The detailed characterization of bioactive macromolecules extracted from aquaculture processing waste provides valuable insights into their physicochemical, biochemical and structural properties.These findings suggest that chitin and chitosan are promising biopolymers due to their stability, antimicrobial properties, and adsorption capabilities. Gelatin demonstrates strong potential for pharmaceutical and food applications due to its gel-forming capacity. Meanwhile, trypsin and chymotrypsin emerge as potent biocatalysts with high enzymatic efficiency. The transformation of aquaculture waste into high-value biomolecules promotes sustainability while enhancing economic viability in multiple industries. This study highlights the significant potentialof these macromolecules, offering avenues for further research and industrial applications.

This study comprehensively characterized bioactive macromolecules extracted from aquaculture processing waste, providing valuable insights into their physicochemical, biochemical and structural properties. The findings highlight the significant potential of these macromolecules for applications in pharmaceuticals, biomedical engineering, food technology, and industrial bioprocessing. The physicochemical analysis revealed that chitin, chitosan, gelatin, trypsin, and chymotrypsin exhibited distinct properties influencing their functional applications. Chitosan demonstrated high solubility and antimicrobial activity, while gelatin exhibited excellent gel strength, making it suitable for pharmaceutical formulations.

The biochemical characterization confirmed the high enzymatic efficiencies of trypsin and chymotrypsin, reinforcing their role as potent biocatalysts. Chitosanexhibited strong antimicrobial properties, while gelatin’s high protein content made it valuable for nutraceutical and pharmaceutical applications. Structural characterization using FTIR analysis confirmed key functional groups indicating strong hydrogenbonding and protein interactions. Morphological analysis using SEM showed that chitin had a compact, fibrous structure, chitosan exhibited a porous morphology, and gelatin formed a smooth, film-like structure, supporting their respective applications in biomaterials and food formulations.

The transformation of aquaculture processing waste into valuable biomolecules presents a sustainable and economically viable approach for industrial applications. Chitin and chitosan emerge as promising biopolymers with high stability, antimicrobial properties, and adsorption capabilities. Gelatin demonstrates strong potential in pharmaceuticals and food industries due to its gel-forming properties, while trypsin and chymotrypsin serve as efficient biocatalysts in protein hydrolysis.

The significance extends beyond mere characterization; it serves asa bridge between extraction and application, ensuring the effective transformation of aquaculture processing waste into high-value bioactive compounds. By demonstratingthe potential of these macromolecules, this study contributes to the advancement of sustainable practices, supporting circular economy principles and reducingenvironmental waste. Through rigorous characterization and evaluation, this work paves the wayfor the integration of aquaculture processing derived biomolecules into various industrial applications, fostering economic growth while promoting environmental sustainability.

These findings reinforce the importance of valorizing aquaculture processing waste, paving the way for future research focused on optimizing extraction methods and exploring novel applications of these macromolecules in various sectors.

### Table1:PhysiologicalPropertiesofBioactiveMacromoleculesfromAquaculture Processing Waste:

| Property | Chitin (Crustacean Exoskeleton) | Chitosan (Deacetylated Chitin) | Gelatin(Fish Skin) | Trypsin(Fish Viscera) | Chymotrypsin (FishViscera) |
| --- | --- | --- | --- | --- | --- |
| pH | 7.3 ±0.3 | 6.1 ±0.4 | 5.3 ±0.2 | 7.5 – 8.5 | 7.8 – 8.2 |
| Moisture Content(%) | 10.3 ±2.2 | 12.4 ±3.1 | 7.8 ±2.3 | 6.4 ±1.7 | 6.4 ±1.7 |
| Ash Content (%) | 1 – 3 | 0.5 – 2 | 0.5 – 1.5 | 0.2 – 1.0 | 0.2 – 1.0 |
| Degreeof Deacetylation (%) | 82.5 ±3.4 | 85.4 ±9.5 | - | - | - |
| Water Solubility(%) | Insoluble | 83.45±6.41 | 94.2 ±1.8 | 100 | 100 |
| Thermal Degradation (°C) | 311.23±23.54 | 246.45±30.54 | 126.62±18.42 | 54.34±6.54 | 54.5 ±6.34 |
| Molecular Weight(kDa) | 743 ±21.3 | 634.47±23.66 | 143.23±12.8 | 24.45±2.34 | 25.63±2.34 |
| Optimum Temperature (°C) | - | - | - | 38.23±3.21 | 37.23±5.21 |
| OptimumpH ForActivity | - | - | - | 7.5 ±1.5 | 7.8 ±1.2 |

Write standard value for these study.

The values presented in this study represent the means obtained from three independent experimental replicates, ensuring reliability and reproducibility of the data. The accompanying ± symbol denotes the standard error (SE), which quantifies the variability of the mean and provides an estimate of the precision of the measurements.

Table.2:BiochemicalPropertiesofExtractedBioactiveMacromolecules from Aquaculture Processing Waste:

| Property | Chitin | Chitosan | Gelatin | Trypsin (FishViscera) | Chymotrypsin (FishViscera) |
| --- | --- | --- | --- | --- | --- |
| ProteinContent (%) | 0.7±0.01 | 0.9±0.01 | 85.6± 9.5 | 91.21± 6.54 | 87.38± 6.21 |
| LipidContent(%) | 0.3 ±0.02 | 0.27± 0.01 | 0.71± 0.43 | 0.52± 0.1 | 0.45± 0.21 |
| Enzymatic Activity(U/mg) | - | - | - | 10543.23±68.75 | 9673.54±34.23 |
| Antimicrobial Activity(MIC, µg/mL) | 123.34±28.34 | 85.23± 14.67 | - | - | - |
| GelStrength (Bloomg) | - | - | 234.45±9.42 | - | - |
| IsoelectricPoint (pI) | 5.7±0.3 | 6.2 ±08 | 5.12± 0.5 | 9.6±1.7 | 8.1±0.3 |

The values presented in this study represent the means obtained from three independent experimental replicates, ensuring reliability and reproducibility of the data. The accompanying ± symbol denotes the standard error (SE), which quantifies the variability of the mean and provides an estimate of the precision of the measurements.

Table3:Fourier-TransformInfraredSpectroscopy(FTIR)FunctionalGroups Identified:

| Wave- number (cm⁻¹) | ChitinFunctional Groups | Chitosan Functional Groups | Gelatin Functional Groups | Proteolytic Enzyme Functional Groups(Trypsin) | ProteolyticEnzyme Functional Groups (Chymotrypsin) |
| --- | --- | --- | --- | --- | --- |
| 3400 – 3450 | O–H&N–H stretching (hydrogenbonds, polysaccharide backbone) | O–H&N–H stretching (hydrogen bonds,amideI) | O–H&N–H stretching (protein structure) | O–H&N–H stretching(amide A, protein secondary structure) | O–H&N–H stretching(amide A, protein structure) |
| 3250 – 3280 | N–H stretching (amideA,protein- like bonds) | N–Hstretching (amideA, protein-like bonds) | N–Hstretching (amideA) | N–Hstretching (amideA) | N–Hstretching (amideA) |
| 2900 – 2960 | C–Hsymmetric&asymmetric stretching (CH₃,CH₂) | C–H symmetric & asymmetric stretching(CH₃, CH₂) | C–H stretching (protein&lipid interaction) | C–Hstretching (protein-lipid complex) | C–Hstretching (protein-lipid complex) |
| 1650 – 1660 | Amide I (C=O stretching-sheet) | Amide I (C=O stretching, β- sheet-helix) | Amide I(C=O stretching, random coil& α-helix) | Amide I (C=O stretching, β- sheet-helix) | Amide I (C=O stretching-sheet & α-helix) |
| 1550 – 1580 | Amide II (N–H bending–N stretching) | Amide II (N–H bending–N stretching) | Amide II (protein secondary structure) | AmideII(protein folding, β-sheet interactions) | AmideII(protein folding, β-sheet interactions) |
| 1400 – 1460 | CH₃bending(alkyl groups, polysaccharide backbone) | CH₃ bending (alkyl groups, chitosan structure) | CH₃ bending (protein interaction, lipid interface) | CH₃bending (protein-lipid complex) | CH₃bending (protein-lipid complex) |
| 1200 – 1250 | C–N stretching (amide III, glycosidicbond) | C–N stretching (amide III, glycosidicbond) | C–Stretching (amide III, random coil structure) | C–N stretching (amide III, α- helixandβ-sheet presence) | C–N stretching (amideIII,α-helix and β-sheet presence) |
| 1050 – 1080 | C–O–Cstretching (glycosidic bond, polysaccharide structure) | C–O–C stretching (glycosidic bond, deacetylated chitin) | C–O–C stretching (protein- carbohydrate interaction) | C–Ostretching (protein conformation changes) | C–Ostretching (protein conformation changes) |

Table 4: Microstructural Analysis (SEM) of Bioactive Macromolecules Extracted from Aquaculture Processing Waste:

[A]Chitin[B]Chitosan[C]Gelatin[D]Trypsin[E]Chymotrypsin.

| Parameter | Chitin | Chitosan | Gelatin | Proteolytic Enzyme (Trypsin) | Proteolytic Enzyme (Chymotrypsin) |
| --- | --- | --- | --- | --- | --- |
| Surface Morphology | Dense,rigid flakes | Porous,fibrous | Smooth, amorphous | Granular, irregular | Granular,slightly aggregated |
| PoreSize(µm) | 3.2±05 | 32.54± 6.43 | 121.41±18.5 | 3.1 ±1.4 | 2.7±1.54 |
| ParticleSize (nm) | 181.22±14.24 | 336.74±38.54 | 460.53±63.42 | 32.56±41.65 | 54.34± 62.54 |

Write standard value for these study.

The values presented in this study represent the means obtained from three independent experimental replicates, ensuring reliability and reproducibility of the data. The accompanying ± symbol denotes the standard error (SE), which quantifies the variability of the mean and provides an estimate of the precision of the measurements.

Fig.1FTIRspectrafortheExtractedBioactiveMoleculesfromAquaculture Processing Waste:

[A]Chitin,[B]Chitosan,[C]Gelatin,[D]Trypsin,and[E]Chymotrypsin.

Fig.2: SEM Images of Bioactive Macromolecules Extracted from Aquaculture Processing Waste:

[A]Chitin[B]Chitosan[C]Gelatin[D]Trypsin[E] Chymotrypsin.

Write the conclusion of these studies.

References:

AlKhawli,F.,Martí-Quijal,F.J.,Ferrer,E.,Ruiz,M.J.,Berrada,H.,Gavahian,M.,Barba, F.J. and de La Fuente, B., 2020. Aquaculture and its by-products as a source of nutrientsandbioactivecompounds.InAdvancesinfoodandnutritionresearch(Vol. 92, pp. 1-33). Academic Press

Anderson,J.L.,Asche,F.,Garlock,T.andChu,J.,2017.Aquaculture:Itsroleinthefuture of food. InWorld agricultural resources and food security: International food security(pp.159-173).EmeraldPublishingLimited.

Bjurström, H., Lind, B. B., & Lagerkvist, A. (2014). Unburned carbon in combustion residuesfromsolidbiofuels.Fuel,117,890-899.

Choudhury,A.,Lepine,C.,Witarsa,F.andGood,C.,2022.Anaerobicdigestionchallenges andresourcerecoveryopportunitiesfromland-basedaquaculturewasteandseafood processingbyproducts: Areview. BioresourceTechnology,354,p.127144.

Coppola, D., Lauritano, C., Palma Esposito, F., Riccio, G., Rizzo, C. and de Pascale, D., 2021.Fishwaste:Fromproblemtovaluableresource.Marinedrugs,19(2),p.116.

Fraga-Corral,M.,Ronza,P.,Garcia-Oliveira,P.,Pereira,A.G.,Losada,A.P.,Prieto,M.A., Quiroga,M.I.andSimal-Gandara,J.,2022.Aquacultureasacircularbio-economy model with Galicia as a study case: How to transform waste into revalorized by- products.TrendsinFoodScience&Technology,119,pp.23-35.

Guru, G. S., Pandey, C., Ali, M., & Thiske, S. (2024). Exploring the Morphological Foundations of Fish Culture : A Review. International Journal of Science, Architecture, Technology, and Environment, 01(05), 69–77.

Goudie, K. J., McCreath, S. J., Parkinson, J. A., Davidson, C. M., &Liggat, J. J. (2023). Investigation of the influence of pH on the properties and morphology of gelatin hydrogels.JournalofPolymerScience,61(19),2316-2332.

Little,D.C.,Newton,R.W.andBeveridge,M.C.M.,2016.Aquaculture:arapidlygrowing andsignificantsourceofsustainablefood?Status,transitionsandpotential.ProceedingsoftheNutritionSociety,75(3),pp.274-286.

Maschmeyer, T., Luque, R., &Selva,M. (2020). Upgradingofmarine (fish and crustaceans) biowaste for high added-value molecules and bio (nano)-materials.Chemical Society Reviews, 49(13), 4527-4563.

O’Kelly,B.C.(2004).Accuratedeterminationofmoisture ontentoforganicsoilsusingthe ovendryingmethod.DryingTechnology,22(7),1767-1776.

Rebouças, J.S.A., Oliveira, F.P.S., Araujo, A.C.D.S., Gouveia, H.L., Latorres, J.M., Martins, V.G., Prentice Hernández, C. and Tesser, M.B., 2023. Shellfish industrial waste reuse.CriticalReviewsinBiotechnology,43(1),pp.50-66.

Reddy, L. H.,Arias,J. L., Nicolas,J., &Couvreur,P.(2012).Magneticnanoparticles:design andcharacterization,toxicityandbiocompatibility,pharmaceuticalandbiomedical applications.Chemicalreviews,112(11),5818-5878.

Rawte , K., Damle, K. L., Thiske , S., Ali , M., Bhatia ,  G.B., Pandey,  C.,  Guru, G. S. (2024). Bioremediation of Pollutants in the Shivnath River: Harnessing Natural Processes for Ecosystem Restoration. Degres Journal, 09 (12), ISSN NO:0376-8163. https://degres.eu/wp-content/uploads/1_1431DEJ.pdf

Shah,F.A.,Ruscsák,K.,&Palmquist,A.(2019).50yearsof scanning gelectronmicroscopy ofbone—acomprehensiveoverviewoftheimportantdiscoveriesmadeandinsights gained into bone material properties in health, disease, and taphonomy.Bone research, 7(1), 15.

Green highlighted not relevant to you’re cited line.

Stevens,J.R.,Newton,R.W.,Tlusty,M.,&Little,D.C.(2018).Theriseofaquacultureby- products: Increasing food production, value, and sustainability through strategic utilisation.MarinePolicy,90,115-124.

Udayakumar, G. P., Muthusamy, S., Selvaganesh, B., Sivarajasekar, N., Rambabu, K., Banat, F.,& Show, P. L. (2021). Biopolymers and composites: Properties, characterization and their applications in food, medical and pharmaceutical industries.Journal of EnvironmentalChemical Engineering,9(4),105322.

References are not sufficient for these studies.