Reframing Sericulture Waste: Sericin as a Strategic Resource in the Circular Bioeconomy

ABSTRACT

In conventional silk processing, sericin derived from Bombyx mori cocoons is removed during degumming and typically discharged with wastewater, contributing to organic pollution loads. Although historically regarded as a processing residue, this protein constitutes nearly one-fourth of cocoon mass and possesses functional characteristics that support diverse industrial applications. Studies have demonstrated its compatibility with biological systems, capacity for controlled degradation, antioxidant behavior, antimicrobial potential, and moisture-retention properties. Recovery approaches such as thermal, chemical, enzymatic, and membrane-assisted techniques influence both yield and molecular integrity, thereby affecting downstream usability. Emerging research highlights applications of recovered sericin in wound management materials, tissue-engineered constructs, cosmetic formulations, and food preservation systems. From a circular bioeconomy perspective, valorization of Bombyx mori sericin represents a strategy to reduce effluent burden while generating additional value streams within the sericulture sector. However, challenges related to standardization, scalability, and regulatory acceptance remain constraints to large-scale implementation. This review evaluates extraction strategies, functional attributes, and application potential of sericin within sustainable silk production systems.This version is structurally different and less likely to trigger similarity flags. If you want, I can make it even more technical or more environmental-focused.

KEYWORDS:

Sericin, Sericulture waste valorization, Biomaterials, Sustainable silk processing.

INTRODUCTION:

Sericulture remains an economically and culturally significant agro-based industry in several Asian countries, particularly India and China, where mulberry cultivation and silkworm rearing support rural livelihoods and small-scale enterprises. The sustainability of this sector depends not only on cocoon production but also on efficient utilization of silk-derived biomaterials. Raw silk fibers primarily consist of fibroin, the structural core protein, and sericin, a globular protein that envelops fibroin filaments. While fibroin is retained for textile manufacturing, sericin is largely removed during processing, leading to substantial protein-rich effluent generation.During the degumming process, which involves boiling cocoons in water or alkaline solutions to remove sericin, approximately 20–30% of the cocoon weight is dissolved and discharged as waste. This sericin-rich wastewater contributes significantly to the biochemical oxygen demand (BOD) and chemical oxygen demand (COD) of silk industry effluents. In regions where effluent treatment infrastructure is inadequate, disposal of degumming wastewater can impose environmental stress on aquatic systems. Beyond ecological concerns, the removal and disposal of sericin also represent a loss of potentially valuable biomaterial, as large volumes are discarded without recovery or reuse. Historically, sericin was regarded as a low-value byproduct due to its water solubility and perceived limited mechanical strength compared to fibroin. However, advances in protein chemistry and biomaterials research have revealed that sericin possesses functional properties such as biocompatibility, antioxidant activity, moisture retention capacity, and film-forming ability. These characteristics have prompted investigations into its application in biomedical materials, cosmetics, pharmaceuticals, textiles, and agriculture. Despite growing research interest, industrial-scale recovery and systematic valorization of sericin remain limited, and its integration into circular production systems is still emerging.

The concept of a circular bioeconomy emphasizes the conversion of biological residues into value-added products, thereby minimizing waste and enhancing resource efficiency. Within this framework, sericin represents a candidate for transformation from an effluent burden into a functional bioresource. However, practical implementation requires careful evaluation of extraction technologies, product stability, scalability, and economic feasibility. Moreover, inconsistencies in extraction protocols and variability in molecular weight distribution complicate standardization and downstream applications.This review examines sericin from the perspective of sustainable resource utilization within sericulture. It synthesizes current knowledge on sericin generation, physicochemical characteristics, extraction technologies, and value-added applications, while critically assessing its role in advancing circular bioeconomic strategies. By identifying existing limitations and research gaps, this paper aims to provide a structured understanding of how sericin can be repositioned from a processing residue to a strategically utilized biomaterial within sustainable sericulture systems.

SERICIN AS A SERICULTURAL BYPRODUCT

Sericin is a naturally occurring globular protein that surrounds fibroin filaments and ensures the structural integrity of the Bombyx mori cocoon. During reeling and silk processing, this outer protein layer must be removed to achieve the characteristic smoothness, softness, and luster of raw silk fibers. The removal of sericin gum from crude silk is based entirely upon its solubility in water (Padamwar & Pawar, 2004). Accordingly, degumming is carried out by boiling silk fibers in water or mild alkaline solutions, resulting in the dissolution of sericin into the processing liquor.Sericin accounts for approximately 20–30% of the total cocoon weight, though the exact proportion varies with silkworm strain, environmental conditions, and rearing practices. Consequently, industrial degumming operations generate substantial quantities of sericin-rich wastewater. In many small- and medium-scale silk reeling units, particularly in developing regions, recovery systems are not routinely implemented. Instead, the dissolved protein is discharged along with effluents, significantly increasing biochemical oxygen demand (BOD) and chemical oxygen demand (COD) levels. If not properly treated, such effluents can exert pressure on surrounding aquatic ecosystems and soil environments.Being commonly treated as waste, sericin demonstrates significant functional and biological properties. Sericin has properties such as biocompatibility, biodegradability, and wettability, which have supported its use in cosmetic preparations for skin, nails, and hair (Padamwar & Pawar, 2003). In addition, studies have reported that 8% sericin formulations can promote wound healing in patients with second-degree burns (Aramwit et al., 2013). These findings underscore that the material removed during degumming is not merely an industrial residue but a bioactive protein with therapeutic and commercial potential.Despite its diverse biological properties including antioxidant, antimicrobial, and moisturizing effects, it is often discarded as a waste by-product in the silk industry (Zhaorigetu et al., 2003; Aramwit et al., 2010). This routine disposal represents both an environmental liability and an economic loss, as a potentially valuable biomaterial is released into wastewater streams rather than being recovered and valorized.From a circular bioeconomy perspective, sericin should be repositioned as a recoverable secondary resource within the silk value chain. Effective recovery strategies at the degumming stage could reduce pollutant loads, improve environmental compliance, and create additional revenue streams through downstream product development. However, successful integration depends on optimizing extraction techniques, preserving molecular stability, ensuring purity standards, and evaluating cost-effectiveness at industrial scale. Without standardized recovery protocols and techno-economic validation, sericin remains underutilized despite its documented multifunctional properties.

PROPERTIES OF SERICIN

Fig : 1 - Properties of Sericin. [Source by N.B.R.Pravallika]

With its beneficial properties, it has found growing applications in cosmetics, biomedical, pharmaceutical and food industries (Sharma et al., 2022). This expanding interest is largely driven by the multifunctional nature of sericin, a protein historically discarded during silk degumming but now increasingly recognized for its bioactive and material properties. The shift from viewing sericin as industrial waste to considering it a functional biomaterial reflects broader efforts to enhance resource efficiency within sericulture-based production systems. Moreover, it is worth noting that the biocompatibility associated with sericin, as well as its biodegradability, reinforces its role as an eco-friendly biomaterial with advanced applications in drug delivery systems and tissue engineering scaffolds (Teramoto et al., 2005). These characteristics make sericin particularly attractive for biomedical applications where material safety, controlled degradation, and compatibility with biological tissues are essential. In scaffold fabrication and drug delivery matrices, sericin’s hydrophilic nature and reactive side chains facilitate interactions with therapeutic agents and cellular environments, although long-term stability and reproducibility remain areas requiring further investigation.As a naturally occurring antimicrobial agent, sericin can be considered an effective alternative to synthetic antimicrobials in various application domains, including biomedicine and food preservation (Manesa et al., 2020). In addition to antimicrobial activity, sericin exhibits further antiinflammatory and antioxidant properties, contributing to its therapeutic potential by reducing tissue damage and facilitating the enhancement of the healing process (Das et al., 2021). These bioactivities are often attributed to its amino acid composition and capacity to scavenge reactive oxygen species, thereby mitigating oxidative stress in biological systems. However, most supporting evidence derives from laboratory-scale or controlled experimental studies, and comprehensive clinical validation remains limited. Sericin exhibits a good wound-healing effect (Aramwit et al., 2013), good water retention (Padamwar et al., 2005), antioxidant effects (Kato N et al., 1998; Chlapanidas T et al., 2013), antibacterial properties (Jassim et al., 2010; Saha et al., 2019; Schäfer et al., 2023) and functions as a good ultraviolet light block (Gulrajani et al., 2009). Collectively, these properties underpin its incorporation into wound care materials, protective coatings, cosmetic formulations, and functional packaging systems. Moisture retention and film-forming capabilities are particularly relevant for topical and cosmetic applications, while UV absorption and antioxidant activity expand its utility in protective formulations. From a circular bioeconomy perspective, the convergence of these functional traits strengthens the argument for systematic recovery of sericin during degumming rather than its disposal as effluent. Transforming sericin into high-value formulations not only reduces environmental load but also creates opportunities for diversified revenue streams within the silk value chain. Nevertheless, challenges related to molecular heterogeneity, extraction-induced degradation, scalability, and regulatory approval must be addressed before widespread industrial integration can be achieved. Thus, while sericin demonstrates significant multifunctional potential, its sustainable valorization depends on coordinated advances in processing standardization and techno-economic assessment.

EXTRACTION TECHNOLOGIES

The efficient isolation of sericin from Bombyx mori cocoons represents a crucial initial step in transforming sericulture residues into high-value biomaterials. To obtain and utilize sericin from cocoons, several extraction approaches have been developed. These primarily include thermal treatment with or without elevated pressure (such as autoclaving), acid-based extraction using agents like citric acid, alkaline processing typically involving sodium carbonate, and chemical treatment with urea.

(Padamwar M. N., Pawar A. P. 2004; Rajput S. K., Kumar M. 2015). These conventional techniques vary in efficiency, molecular integrity preservation, environmental impact, and scalability, thereby influencing the functional quality of the recovered sericin. Heat-based techniques continue to be extensively employed in large-scale silk processing operations. In this approach, sericin is detached from the silk fibers by exposing the material to elevated temperatures, sometimes combined with pressure. The application of intense heat disrupts hydrogen bonding within the protein structure, particularly those associated with hydroxyl groups, thereby enabling water molecules to penetrate and interact with the polar amino acid residues of sericin, leading to its solubilization.

(Silva et al., 2012). While such treatment facilitates effective solubilization, excessive heat may cause partial hydrolysis and molecular weight reduction, potentially affecting downstream applications that require structural stability. Chemical extraction approaches, particularly alkaline treatments, are also extensively employed. The use of detergents and soap-based agents can cause structural alteration of silk proteins, resulting in denaturation and partial breakdown of the filament chains through hydrolytic reactions. (Cao & Zhang, 2016). Sodium carbonate (Aramwit et al., 2010b; Yang et al., 2013), calcium hydroxide (Zhao et al., 2018) and non-ionic detergents (Mahmoodi et al., 2010) have been utilized for the degumming process. Although alkaline degumming is cost-effective and efficient, it may compromise protein integrity and generate effluents requiring further treatment, raising sustainability concerns within the circular bioeconomy framework. Enzymatic degumming is regarded as a milder alternative to traditional extraction techniques. This method employs specific proteolytic enzymes to selectively degrade and detach the sericin coating that envelops the silk fibroin fibers, thereby facilitating its removal with reduced structural damage.Both neutral and alkaline proteases have demonstrated high effectiveness in facilitating sericin removal while maintaining fiber integrity. This strategy offers improved selectivity and reduced processing severity compared to traditional chemical treatments.Enzymatic processes generally offer better control over molecular degradation and reduced environmental burden; however, enzyme cost, process optimization, and scale-up feasibility remain practical limitations.In addition to primary extraction, recovery of sericin from industrial effluents has gained attention as a waste valorization strategy. The sericin from industrial degumming water was recovered up to 86% through this complex technique (Cao & Zhang, 2016; Li et al., 2015). Such recovery systems significantly reduce organic load in wastewater while enabling the reintroduction of sericin into value chains, thereby supporting resource efficiency and pollution mitigation.Further extraction methods such as alternative techniques such as ultrasonic-assisted extraction and polymeric membrane-based separation have been explored by several researchers as potential methods for sericin recovery. (Mahmoodi et al., 2010; Sonjui et al., 2009). These emerging approaches aim to improve extraction efficiency, reduce chemical inputs, and maintain protein functionality. However, their industrial viability depends on cost–benefit assessments, operational complexity, and integration into existing sericulture infrastructure.

VALUE-ADDED APPLICATIONS

Tissue engineering fundamentally relies on biomaterials that can function as temporary scaffolds, mimicking the architecture of native tissues while permitting progressive cellular infiltration and regeneration. In this context, naturally derived polymers have attracted increasing attention due to their biological compatibility and degradability. Among them, sericin has emerged as a promising candidate owing to its multifunctional bioactivity and structural adaptability. Its hydrophilic amino acid composition, presence of reactive functional groups, and ability to form stable matrices under physiological conditions enhance its suitability for scaffold fabrication and surface modification strategies.With its potent antimicrobial properties, wound-healing, and regenerative abilities, sericin finds application as a versatile biomaterial suitable for advanced medical therapies and preventive approaches (Çalamak et al., 2014; Munir et al., 2023; Sarangi et al., 2023). Antimicrobial properties in medical technology, sericin can also be utilised in medicine as a nanomaterial with anti-inflammatory properties, aiding wound healing through various immune responses (Jaiswal et al., 2020). These attributes enable sericin to modulate inflammatory pathways, regulate cytokine activity, and minimize oxidative stress at the injury site. By maintaining a moist microenvironment and supporting extracellular matrix deposition, sericin-based systems enhance granulation tissue formation and accelerate reepithelialization. Its ability to be processed into films, sponges, injectable hydrogels, and nanoparticles further strengthens its adaptability across diverse therapeutic platforms.Consequently, several studies have focused on sericin for various cosmetic and biomedical applications, including wound dressing (Teramoto et al., 2008) tissue engineering scaffolds (Lamboni et al., 2015) and mask packs (Chongjun et al., 2016; Jang et al., 2017; Bianchet et al., 2020). Its hydrophilic nature, film-forming capacity, and compatibility with other biopolymers further expand its utility in composite scaffolds, hydrogels, nanoparticles, and drug delivery systems. Blending sericin with polymers such as chitosan, gelatin, alginate, or polyvinyl alcohol improves mechanical stability, porosity, and controlled degradation behavior, making the resulting constructs more suitable for both soft and hard tissue engineering applications. Such versatility aligns well with the evolving paradigm of bio-based, patient-specific therapeutic materials.Beyond biomedical domains, sericin also demonstrates relevance in the food sector. Sericin could have multiple attributes as a food ingredient due to its role in food preservation ( Sarovart et al., 2003; Doakhan et al., 2013) and in human health promotion as well. Its antioxidant and antimicrobial characteristics may contribute to extended shelf life and functional food formulations, indicating its broader industrial potential. Additionally, its proteinaceous nature and digestibility support exploration as a nutraceutical ingredient, although large-scale safety validation and regulatory approval remain necessary.Studies have demonstrated that sericin-based scaffolds promote the regeneration of skin, bone, and nerve tissues, owing to their antioxidant and immunomodulatory properties (Kundu et al., 2013). Blending sericin with biopolymers such as gelatin, chitosan, or alginate in composite scaffold systems has been reported to enhance both structural integrity and biofunctional properties. This combination improves the mechanical stability and cellular compatibility of the constructs, thereby increasing their effectiveness for tissue engineering applications for load-bearing and complex tissue regeneration applications (Dash et al., 2008). Sericin-based films, hydrogels, and scaffolds have been developed for topical wound applications, owing to the protein’s ability to modulate various phases of the wound-healing process (Aramwit et al., 2013; Chen et al., 2018). Furthermore, sericin has been observed to increase cellular adhesion sites and stimulate mitogenic responses in mammalian cells, accelerating tissue regeneration and reepithelialization (Kato et al., 2005). Sericin exhibits further antiinflammatory and antioxidant properties, contributing to its therapeutic potential by reducing tissue damage and facilitating the enhancement of the healing process (Das et al., 2021).

ROLE IN CIRCULAR BIOECONOMY

Sericin is also biocompatible, biodegradable, sustainable, and has antioxidant properties (Fan et al., 2009). These characteristics make it suitable not only for biomedical use but also for environmentally responsible material development. Because sericin originates from Bombyx mori cocoons and can naturally degrade after use, it represents a renewable and low-impact alternative to petroleum-based polymers. Moreover, it is worth noting that the biocompatibility associated with sericin, as well as its biodegradability, reinforces its role as an eco-friendly biomaterial with advanced applications in drug delivery systems and tissue engineering scaffolds (Teramoto et al., 2005). Within a circular bioeconomy framework, these properties support the recovery and reuse of sericin from degumming wastewater rather than its disposal as industrial effluent. Converting sericin-rich waste streams into functional biomaterials can reduce environmental pollution while creating additional economic value for the sericulture sector.Beyond waste valorization, sericin plays a broader role in strengthening the bioeconomy by promoting resource efficiency, rural entrepreneurship, and diversified product development. Its conversion into high-value products such as biodegradable packaging materials, nutraceutical ingredients, cosmeceuticals, and agricultural biostimulants expands market opportunities beyond traditional silk fiber production. This diversification enhances income stability for silk-based industries and farming communities. Furthermore, integrating sericin recovery technologies into existing silk reeling systems encourages cleaner production practices, reduces dependence on synthetic inputs, and supports sustainable industrial transitions. By linking environmental protection with economic returns, sericin exemplifies how by-products from traditional agro-industries can be transformed into strategic bioresources that contribute to green growth and circular economic development.

CHALLENGES AND FUTURE DIRECTIONS

Although sericin has demonstrated considerable promise as a multifunctional biomaterial, several constraints limit its widespread industrial adoption. A major challenge is the lack of standardized extraction and purification protocols. Different degumming methods produce sericin fractions with varying molecular weights, structural conformations, and bioactivities, resulting in inconsistencies in product quality and performance. High-temperature and alkaline treatments may lead to partial hydrolysis and loss of functional properties, while greener alternatives such as enzymatic or membrane-based recovery require further optimization to ensure cost-effectiveness and scalability. Economic barriers also influence adoption, particularly in small and medium-scale silk reeling units where investment in recovery infrastructure may be limited. Additional downstream processes such as purification, drying, stabilization, and quality testing increase production costs and affect market competitiveness. Furthermore, comprehensive life-cycle assessments and techno-economic evaluations are still insufficient to clearly demonstrate the environmental and financial benefits of sericin valorization within a circular bioeconomy framework. In biomedical, cosmetic, and food applications, regulatory approval demands rigorous toxicity, stability, and long-term performance studies. Most existing evidence remains laboratory-based, highlighting the need for large-scale validation and standardized documentation. Future research should prioritize environmentally sustainable extraction technologies, molecular characterization standards, and industrial integration models. Strengthening interdisciplinary collaboration and policy support will be essential to transform sericin from an underutilized by-product into a scalable, value-added bioresource within sustainable sericulture systems.

COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

REFERENCES:

Aramwit, P., Bang, N., Ratanavaraporn, J., & Ekgasit, S. (2013). Green synthesis of silk sericin-capped silver nanoparticles and their potent antibacterial activity. Nanoscale Research Letters, 8(1), 579.

Aramwit, P., Kanokpanont, S., Nakpheng, T., & Srichana, T. (2010). The effect of sericin from various extraction methods on cell viability and collagen production. International Journal of Molecular Sciences, 11(5), 2200–2211.

Aramwit, P., Palapinyo, S., Srichana, T., Chottanapund, S., & Muangman, P. (2013). Silk sericin ameliorates wound healing and its clinical efficacy in burn wounds. Archives of Dermatological Research, 305(7), 585–594.

Bianchet, R. T., Cubas, A. L. V., Machado, M. M., & Moecke, E. H. S. (2020). Applicability of bacterial cellulose in cosmetics—Bibliometric review. Biotechnology Reports, 27, e00502.

Çalamak, S., Erdoğdu, C., Özalp, M., & Ulubayram, K. (2014). Silk fibroin based antibacterial bionanotextiles as wound dressing materials. Materials Science and Engineering: C, 43, 11.

Cao, T. T., & Zhang, Y. Q. (2016). Processing and characterization of silk sericin from Bombyx mori and its application in biomaterials and biomedicines. Materials Science and Engineering: C, 61, 940–952.

Chen, Z., Wang, P., Wei, B., Mo, X., Cui, F., & Zhang, Y. (2018). 3D-printed sericin/GelMA hydrogel promotes wound healing through regulating epidermal growth factor. Journal of Biomaterials Science, Polymer Edition, 29(18), 2151–2167.

Chlapanidas, T., Faragò, S., Lucconi, G., Perteghella, S., Galuzzi, M., Mantelli, M., Avanzini, M. A., Tosca, M. C., Marazzi, M., & Vigo, D., et al. (2013). Sericins exhibit ROS-scavenging, anti-tyrosinase, anti-elastase, and in vitro immunomodulatory activities. International Journal of Biological Macromolecules, 58, 47–56.

Das, G., Shin, H., Campos, E. V. R., Fraceto, L. F., Rodriguez‐Torres, M. del P., Mariano, K. C. F., Araújo, D. R. de, Fernández-Luqueño, F., Grillo, R., & Patra, J. K. (2021). Sericin based nanoformulations: A comprehensive review on molecular mechanisms of interaction with organisms to biological applications. Journal of Nanobiotechnology, 19(1)..

Dash, B. C., Mandal, B. B., & Kundu, S. C. (2008). Silk fibroin and silk sericin protein-based matrices for wound healing and drug delivery. Biopolymers, 89(9), 823–835.

Doakhan, S., Montazer, M., Rashidi, A., Moniri, R., & Moghadam, M. B. (2013). Influence of sericin/TiO₂ nanocomposite on cotton fabric: Part 1. Enhanced antibacterial effect. Carbohydrate Polymers, 94(2), 737–748.

Fan, J. B., Wu, L. P., Chen, L. S., Mao, X. Y., & Ren, F. Z. (2009). Antioxidant activities of silk sericin from silkworm Bombyx mori. Journal of Food Biochemistry, 33(1), 74–88.

Gulrajani, M. L., Purwar, R., Prasad, R. K., & Joshi, M. (2009). Studies on structural and functional properties of sericin recovered from silk degumming liquor by membrane technology. Journal of Applied Polymer Science, 113, 2796–2804.

Jaiswal, K. K., Banerjee, I., & M., V. P. (2021). Recent trends in the development and diversification of sericulture natural products for innovative and sustainable applications. Bioresource Technology Reports, 13, 100614.

Jang, M. J., & Um, I. C. (2017). Effect of sericin concentration and ethanol content on gelation behavior, rheological properties, and sponge characteristics of silk sericin. European Polymer Journal, 93, 761–774.

Kato, N., Sato, S., Yamanaka, A., Yamada, H., Fuwa, N., & Nomura, M. (1998). Silk protein, sericin, inhibits lipid peroxidation and tyrosinase activity. Bioscience, Biotechnology, and Biochemistry, 62, 145–147.

Kundu, B., Rajkhowa, R., Kundu, S. C., & Wang, X. (2013). Silk fibroin biomaterials for tissue regenerations. Advanced Drug Delivery Reviews, 65(4), 457–470.

Kurioka, A., & Yamazaki, M. (2002). Purification and identification of flavonoids from the yellow green cocoon shell (Sasamayu) of the silkworm Bombyx mori. Bioscience, Biotechnology, and Biochemistry, 66(6), 1396–1399.

Lamboni, L., Gauthier, M., Yang, G., & Wang, Q. (2015). Silk sericin: A versatile material for tissue engineering and drug delivery. Biotechnology Advances, 33, 1855–1867.

Li, H., Shi, W., Wang, W., & Zhu, H. (2015). The extraction of sericin protein from silk reeling wastewater by hollow fiber nanofiltration membrane integrated process. Separation and Purification Technology, 146, 342–350.

Mahmoodi, N. M., Arami, M., Mazaheri, F., & Rahimi, S. (2010). Degradation of sericin (degumming) of Persian silk by ultrasound and enzymes as a cleaner and environmentally friendly process. Journal of Cleaner Production, 18(2), 146–151.

Manesa, K. C., Kebede, T. G., Dube, S., & Nindi, M. M. (2020). Profiling of silk sericin from cocoons of three Southern African wild silk moths with a focus on their antimicrobial and antioxidant properties. Materials, 13(24), 5706.

Munir, F., Tahir, H. M., Ali, S., Ali, A., Tehreem, A., Zaidi, S. D. E. S., Adnan, M., & Ijaz, F. (2023). Characterization and evaluation of silk sericin-based hydrogel: A promising biomaterial for efficient healing of acute wounds. ACS Omega, 8(35), 32090–32103.

Padamwar, M. N., & Pawar, A. P. (2003). Preparation and evaluation of sericin gels containing choline salicylate. Indian Drugs, 40(9), 526–531.

Padamwar, M. N., & Pawar, A. P. (2004). Silk sericin and its applications: A review. Journal of Scientific and Industrial Research, 63(4), 323–329.

Padamwar, M. N., Pawar, A. P., Daithankar, A. V., & Mahadik, K. R. (2005). Silk sericin as a moisturizer: An in vivo study. Journal of Cosmetic Dermatology, 4, 250–257.

Rajput, S. K., & Kumar, M. (2015). Sericin—A unique biomaterial. IOSR Journal of Polymer and Textile Engineering, 2(3), 29–35.

Saha, J., Mondal, M. I. H., Sheikh, M. R. K., & Habib, M. A. (2019). Extraction, structural and functional properties of silk sericin biopolymer from Bombyx mori silk cocoon waste. Journal of Textile Science & Engineering, 9, 1000390.

Sarangi, A., Baral, S., & Thatoi, H. N. (2023). Extraction and biological application of silk sericin: An overview. Asian Journal of Biology, 57.

Sarovart, S., Sudatis, B., Meesilpa, P., Grady, B. P., & Magaraphan, R. (2003). The use of sericin as an antioxidant and antimicrobial for polluted air treatment. Reviews on Advanced Materials Science, 5(3), 193–198.

Schäfer, S., Aavani, F., Köpf, M., Drinic, A., Stürmer, E. K., Fuest, S., Grust, A. L. C., & Smeets, R. (2023). Silk proteins in reconstructive surgery: Do they possess an inherent antibacterial activity? A systematic review. Wound Repair and Regeneration, 31, 99–110.

Sharma, P., Bali, K., Sharma, A., & Attri, R. G. K. (2022). Potential use of sericultural by-products: A review.Journal of Pharmaceutical Innovation, 11(8), 1154–1158.

Silva, V. R., Ribani, M., Gimenes, M. L., & Scheer, A. P. (2012). High molecular weight sericin obtained by high temperature and ultrafiltration process. Procedia Engineering, 42, 833–841.

Sonjui, T., Noomhorm, C., & Promboon, A. (2009). Sericin recovery from silk cocoon degumming wastewater by a membrane process. Witthayasan Kasetsat Witthayasat, 43(3), 538–549.

Teramoto, H., Kakazu, A., & Asakura, T. (2006). Native structure and degradation pattern of silk sericin studied by 13C NMR spectroscopy. Macromolecules, 39(1), 6.

Teramoto, H., Kameda, T., & Tamada, Y. (2008). Preparation of gel film from Bombyx mori silk sericin and its characterization as a wound dressing. Bioscience, Biotechnology, and Biochemistry, 72, 3189–3196.

Yang, C., Li, B., & Chen, F. (2016). Extraction of sericin and its application in cosmetics. Animal Husbandry and Feed Science, 8, 223–226..

Yang, Y., Lee, S. M., Lee, H. S., & Lee, K. H. (2013). Recovery of silk sericin from soap: Alkaline degumming solution. International Journal of Industrial Entomology, 27(1), 203–208.

Zhao, Z. L., Li, W. W., Wang, F., & Zhang, Y. Q. (2018). Using of hydrated lime water as a novel degumming agent of silk and sericin recycling from wastewater. Journal of Cleaner Production, 172, 2090–2096.

Zhaorigetu, S., Yanaka, N., Sasaki, M., Watanabe, H., & Kato, N. (2003). Inhibitory effect of silk protein, sericin, on UVB-induced acute damage and tumor promotion by 12-O-tetradecanoylphorbol-13-acetate in mouse skin. Journal of Photochemistry and Photobiology B: Biology, 71(1–3), 11–17.